THERMODYNAMICS OF LIQUID NITROGEN SOLUTIONS IN CHROMIUM

L.A. Bolshov, S.K. Korneichuk

Vologda State University, Russia, Vologda

Abstract: A simple theory of thermodynamic properties of liquid nitrogen solutions in Fe-Cr alloys is proposed. The theory based on the lattice model of the considered solutions. The model assumes a FCC lattice. In the lattice sites of this lattice are the atoms of Fe and Cr. Nitrogen atoms are located in octahedral interstices. The nitrogen atom interacts only with the metal atoms located in the lattice sites neighboring to this atom. It is assumed that the energy of this interaction depends neither on the composition nor on the temperature. It is supposed that the solution in the Fe-Cr system is perfect. Within the framework of the proposed theory a relationship is obtained that expresses the value of the Sieverts law constant for the solubility of N in liquid Cr through the similar constant for the solubility of N in liquid Fe and the Wagner N-Cr interaction coefficient in liquid Fe. A relationship is also obtained which expresses the partial enthalpy of nitrogen dissolution in liquid Cr through the similar quantity for N in liquid Fe and Wagner N-Cr interaction coefficient in liquid Fe. A formula deduced that establishes a connection between the Wagner N-Fe interaction coefficient in liquid Cr and N-Cr interaction coefficient in liquid Fe. Using the formulas obtained the value of the Sieverts law constant for the solubility of nitrogen in liquid Cr, the enthalpy of dissolution of N in liquid Cr and the value of the Wagner N-Fe interaction coefficient in liquid Cr extrapolated to a temperature of 1873 K are calculated. The results of the calculation are compared with the results of the experimental study of the solubility of nitrogen in liquid Cr carried out by different researchers using different methods. The result of the theory are in the best agreement with experimental data obtained by the sampling method (F. Ishii, Ya. Iguchi, Sh. Ban-ya, 1986).The values of the Wagner N-N interaction coefficient in liquid Cr and liquid Fe are discussed.

Keywords: thermodynamics, statistical mechanics, solutions, nitrogen, chromium, iron, activity coefficient, enthalpy, Wagner interaction coefficient, Sieverts law.

REFERENCES

1. Dumas M. Recherches sur la composition de l'eau (1) // Annales de chemie et de physique. 3 sèrie. - 1843. – T.8. – P.189-207.
2. Sieverts A. Zur Kenntis der Okklusion und Diffusion von Gasen in Metalle. // Zeitschrift für physikalische Chemie. – 1907. - Bd. 60. – Nr. 2. - S. 129-201.
3. Humbert J.C., Elliott J.F. The solubility of nitrogen in liquid Fe-Cr-Ni alloys // Transactions of the Metallurgical Society of AIME. -1960. –Vol. 218.- No. 10 –Pp. 1076-1088.
4. Ishii F., Iguchi Ya., Ban-ya Sh. Solubility of nitrogen in liquid chromium and chromium-iron alloys. // Transactions of the Iron and Steel Institute of Japan. – 1986. – Vol. 26. - No.2. – Pp. 128-132.
5. Pomarin Yu. M., Grigorenko G.M., Sherevera A.V. Absorption of nitrogen by high-chromium melts and liquid chromium at elevated pressure. // Proceedings of the USSR Academy of Sciences. Metals (Izvestia AN SSSR. Metally) – 1990.- No.5. –Pp. 40-45.
6. Siwka J. Solubility of nitrogen in liquid chromium. // Archives of Metallurgy. – 1998. –Vol. 43. – No.1. – Pp. 67-82.
7. Kor G.J.W. The solubility of nitrogen in liquid manganese. // Metallurgical and Materials Transactions. B. – 1978. – Vol. 9 - No. 2.–Pp. 97-99.
8. Blossey R.G., Pehlke R.D. Solubility of nitrogen in liquid Co alloys. // Transactions of the Metallurgical Society of AIME. – 1966. –Vol. 236. - No.1 – Pp.28-32.
9. Stomakhin A. Ya., Bayer P., Polyakov A. Yu. Solubility of nitrogen in liquid nickel and nickel alloys with chromium, molybdenum and tungsten. // Proceedings of the USSR Academy of Sciences. (Izvestiya AN SSSR. Metally) – 1965. - No.4. – Pp.37-45.
10. Abdulrahman R.F., Hendry A. The solubility of nitrogen in liquid pure nickel. // Metallurgical and Materials Transactions. B. -2001.- Vol. 32. -No.6 – Pp. 1095-1101.
11. Kowanda C., Speidel M.O. Solubility of nitrogen in liquid nickel and binary Ni-Xi alloys( Xi=Cr, Mo, W, Mn, Fe, Co) under elevated pressure // Scripta Materialia. – 2003. – Vol. 48. - No. 8 – Pp. 1073-1078.
12. Rashev Ts. High nitrogen steel. Metallurgy under pressure. – Sofia: Publishing house of the Bulgarien Academy of Sciences «M. Drinov». – 1995. – 268p.
13. Yavoysky V.I., Svyazhin A.G., Chursin G.M., Vishkarev A.F. Thermodynamics and kinetics of the interaction of nitrogen with iron melts. In the collection “Reports of Soviet scientists in the third Soviet-Japanese symposium on physico-chemical fundamentals of metallurgical processes” – Moscow: A.A. Baykov Institute of Metallurgy. – 1971.
14. Lakomsky V.I., Crigorenko G.M., Torkhov G.F., Pomarin Yu.M. Effect of chromium and nickel on the solubility of nitrogen in iron alloys at high temperatures. Ibid.
15. Bolshov L. A. On the solubility of nitrogen in liquid multicomponent iron alloys with transition metals. // Proceedings of the higher educational institutions. Ferrous metallurgy. (Izvestiya vuzov. Chernaya metallurgiya). — 1982. — No. 1 . — Pp. 8-10.
16. Bolshov L. A. Statistical theory of multicomponent and low-concentration alloys. Thesis for the degree DSc (Physics and Mathematics) — Moscow: Moscow State University, 1991. — 496 p.
17. Wagner C. Thermodynamics of Alloys. — Moscow: Metallurgizdat Publ., 1957. — 179 p.
18. Grigoryan V. A., Belyanchikov L. N., Stomakhin A. Ya. Theoretical fundamentals of electric steelmaking processes. — Moscow: Metallurgizdat Publ., 1987. — 272 p.
19. Lupis C. H. P. Chemical Thermodynamics of Materials. — Moscow: Metallurgizdat Publ., 1989. — 504 p.
20. Turnock P. H, Pehlke R. D. The solubility of nitrogen in multicomponent liquid iron alloys. // Transactions of the Metallurgical Society of AIME. — 1966. — Vol. 236. — No. 11. — Pp. 1540-1547.
21. Grigoryan V. A., Stomakhin A. Ya., Utochkin Yu. I., Ponomarenko A. G., Belyanchikov L. N., Kotelnikov G. I., Ostrovsky O. I. Physico-chemical calculations of electric steelmaking processes. — Moscow: Moscow Institute of Steel and Alloys, 2007. — 318 p.
22. Sully A., Brandes E. Chromium. — Moscow: Metallurgiya Publ., 1971. — 360 p.
23. Marchenko L. G., Guglya A. G. Computer simulation of transient layer chemical composition in Cr-N films obtained by ion beam assisted deposition. // Issues of Atomic Science and Technology (Voprosy atomnoi nauki I tekhniki). — 2001. — No. 4 — Pp. 137-139.
24. Rashev Ts., Ivanov R., Sarivanov L., Andreev Ch. Investigation of the nitrogen solubility in iron-chromium alloys under pressure. // Metallurgy (Sofia). — 1976. — Vol. 31. — No. 6. — Pp. 8-10.
25. Bolshov L. A., Bogdanov V. I., Gorbunov V. A. Wagner’s nitrogen-nitrogen interaction coefficient in iron based liquid alloys. // Journal of Physics: Conference Series. — 2008. — Vol. 98. — 032019.
26. Oda K., Fujimura H., Ino H., Local interactions in carbon-carbon and carbon-M (M: Al, Mn, Ni) atomic pairs in FCC γ-iron. // Journal of Physics: Condensed Matter. — 1994. — Vol. 6. — No. 3. — Pp. 679-692.
27. Bolshov L. A., Bogdanov V. I., Gorbunov V. A. Thermodynamic analysis of nitrogen solubility data in gamma-iron under high pressure. // Physics of Metals and Metallography (Fizika metallov i metallovedenie). — 2009. — Vol. 107. — No. 6. — Pp. 591-598.
28. Nechaev Yu. S., Omelchenko A. V. Solubility of molecular nitrogen in austenite. // Journal of Physical Chemistry (Zhurnal fizicheskoi khimii). — 1995. — Vol. 69. — No. 9. — Pp. 1556-1561.

Information about the authors:

L. A. Bolshov, DSc (Physics and Mathematics), Professor of the Department of Higher Mathematics ([labolshov@mail.ru](mailto:labolshov@mail.ru))

S. K. Korneichuk, Candidate of Sciences (Physics and Mathematics), Docent, Head of the Department of Physics ([korn62@mail.ru](mailto:korn62@mail.ru))

Reseived